## Slide 1: Progress Update
10.20.2026

## Slide 2: Part 1: Lippmann-Schwinger to TFA
Goal: I want to express the following TFA equation using Lippmann-Schwinger operators, i.e., define and in terms of these operators.
Reason: I want to explore a TFA-adjacent framework which allows for online FFT-acceleration. If I can express the TFA equation above using the Lippmann-Schwinger operators, it will be easier to perform a clear comparison between the two schemes.

## Slide 3: Derivation: LS to TFA (1)
Starting with the constitutive law, compatibility, and equilibrium:
Define a polarization stress (where is the stiffness of a homogeneous reference material):
Rewrite the equilibrium equation with the polarization stress:

## Slide 4
Rearrange the equation to put the polarization stress on the RHS:
Define the RHS as a force, i.e., :
Derivation: LS to TFA (2)
Because this is a homogeneous material subject to a force , we can employ the Green’s operator:
We can define the strain as:

## Slide 5
Bring the polarization stress back:
Derivation: LS to TFA (3)
Then bring the original stress back (and pull the negative sign out):
Define a new operator (expressed acting on some tensor ):
Then we have:
This is the Lippmann-Schwinger equation

## Slide 6
Plug in the definition for stress:
Derivation: LS to TFA (4)
Rearrange:
Move the total strain () term to the LHS:
Define a new operator (expressed acting on some tensor ):

## Slide 7
Then we have:
Derivation: LS to TFA (5)
Assuming the operator is invertible:
Apply the TFA assumption of constant eigenstrain in partition :
Then we have:

## Slide 8
Define two new tensors (expressed acting on some tensor ):
Derivation: LS to TFA (6)
Then we have:
Take the average of both sides over partition :
This is the TFA form expressed through Lippmann-Schwinger operators !

## Slide 9
We now have a clear expression for the and TFA tensors in terms of the Lippmann-Schwinger operators:
Derivation: LS to TFA (7, Final)
Where:

## Slide 10: Part 2: Lippmann-Schwinger to Constant Polarization
Goal: Starting from the Lippmann-Schwinger equation, derive a TFA-like scheme which instead assumes constant polarization within each partition. Express the tensors of this new scheme in the following form (where refers to constant polarization, and will be introduced later):
Reason: If partitions are uniform, this will allow us to use online FFT acceleration with complexity, with being the number of partitions. Expressing the equation in the form above will allow for direct comparison with the TFA tensor operators.

## Slide 11: Derivation: LS to CP (1)
Starting with the Lippmann-Schwinger equation:
Where:
Apply the assumption of constant polarization stress in partition :

## Slide 12: Derivation: LS to CP (2)
From its definition, the polarization stress for some is expressed as:
Plug the Lippmann-Schwinger equation in for :
Problem (commonly known): The LHS of the above equation must be constant for , but the RHS might not be. Therefore, simultaneously requiring both constant polarization stress and pointwise satisfaction of the Lippmann-Schwinger equation is not always possible.

## Slide 13: Derivation: LS to CP (3)
Solution (also commonly known): Instead, we can assert that the Lippmann-Schwinger equation be satisfied only through partition averages, a relaxation of the pointwise requirement. So, rather than requiring that:
For all , we instead require that:
Within each partition .
This is different from the partition averaging of TFA, which is performed after the pointwise Lippmann-Schwinger equation is already satisfied.

## Slide 14: Derivation: LS to CP (4)
Now, we want to define the polarization stress in terms of the partition averaged strains . To do this, we must first solve the polarization stress for . Restating the polarization stress definition for some :
Solve for (assuming we choose the homogeneous reference stiffness such that exists):
Average over partition :

## Slide 15: Derivation: LS to CP (5)
Then, solve for the polarization stress (assuming exists):
This expression is very messy; we can define some quantities to organize it:
Where the subscript denotes a partition-wise constant field representation. Then, we have:
There’s probably a good way to explain what these two terms mean physically.

## Slide 16: Derivation: LS to CP (6)
Plug this expression back into the partition averaged Lippmann-Schwinger equation:
Move the total strain term to the LHS:
To get rid of the sum notation, we can introduce the following quantities:

## Slide 17: Derivation: LS to CP (7)
Since the product if , we have:
To clean the notation a bit, define a new operator:
Then we have:

## Slide 18: Derivation: LS to CP (8)
Assuming the operator is invertible:
Define another new operator (expressed acting on some tensor ):
Then we have:

## Slide 19: Derivation: LS to CP (9)
To make the comparison with TFA more explicit, we can plug the definition back into the previous equation:
Pull the sum out:

## Slide 20
Define two new tensors (expressed acting on some tensor ):
Derivation: LS to CP (10)
Then we have:
This is a TFA-like form !
We don’t need to take the average of each term over partition anymore, since they are already partition-wise constant. Evaluate each term at partition :

## Slide 21
We now have a clear expression for the and tensors in terms of the Lippmann-Schwinger operators:
Derivation: LS to CP (11, Final)
Where:
Here, denotes the evaluation of the field within partition . No averaging is required, since the terms are already constant in each partition.

## Slide 22: Final Comparison: TFA vs. CP
TFA | CP
TFA | CP

## Slide 23: Final Comparison: TFA vs. CP (Operators)
TFA | CP
TFA | CP
(for

## Slide 24: Final Comparison: TFA vs. CP (Lippmann-Schwinger)
TFA | CP
TFA | CP
To achieve the FFT acceleration, these are the equations we must solve online.

## Slide 25: Thoughts
For the constant polarization scheme, neither strain, nor eigenstrain, are ever assumed constant within each partition. Theoretically, it also allows for multiple material states per partition.
The Lippmann-Schwinger version of the TFA equations shown on the previous slide could also be accelerated using FFT but would only achieve complexity rather than (where is the number of voxels and is the number of partitions). It is unclear to me how that would provide any advantage over standard FFT schemes. The constant polarization scheme, however, achieves .
Many of the ideas in this derivation have been employed before (namely, constant polarization FFT schemes). However, although I’m still reading many papers and familiarizing myself with what’s out there, I can at least confidently say that I haven’t encountered this full derivation anywhere. I also haven’t seen the constant polarization scheme expressed in terms of TFA operators anywhere either. I am still learning though, and I will keep reading other related papers !

## Slide 26: Part 3: Results - Problem Setting
This problem setting aligns the material interfaces perfectly with both the voxels and partitions. It’s an easy toy problem to test out the framework.
I still apply the same loading conditions as the first example from the EBH paper.
elements
partitions

## Slide 27: Results - Stress Contour
Basic FFT solver on the fine grid.
The proposed constant polarization scheme.
Basic FFT solver on the coarse grid.
Standard TFA scheme.
I compare with the basic FFT schemes. They are known for strong ringing near the material interfaces. There are more complex schemes that improve this, I just haven’t implemented them.

## Slide 28: Results - Stress-Strain Curve
They all seem to perform similarly.

## Slide 29: Results - Timing Comparison
I calculated the average online time of 5 runs for each scheme. The results are as follows:
Fine grid FFT:
Coarse grid FFT:
Proposed constant polarization:
TFA:
The constant polarization scheme is the fastest. The gains vs. TFA and the fine grid FFT solver only improve as the number of partitions increases.
Note: TFA performs the best, by far, for smaller partition counts.

## Slide 30: Closing Thoughts / Going Forward
The constant polarization framework should theoretically work even when partitions contain multiple material states. This is important, because not all RVE geometries will conform well to the requirement of both uniform voxels and uniform partitions (where each partition is a uniform group of voxels). I want to try an example of this.
We solve the Lippmann-Schwinger version of the equations online to achieve FFT acceleration. There is no offline calculation. Therefore, the number of partitions in each RVE can be easily updated during the online simulation (assuming the above point regarding multiple material states per partition holds). Is it possible that we could think of an adaptive scheme where the derived TFA-like operators ( and ) are used for low partition counts, and the Lippmann-Schwinger equation is solved for high partition counts ? This would make use of the complexity at high partition counts, and the complexity at low partition counts (which is actually significantly faster in that regime, due to not having to perform the FFT and IFFT).

## Slide 31: Thanks !